## Slide 1: Axial shortening in high rise buildings
Cambridge CSIC
John Parker
09.09.14

## Slide 2: Axial shortening
Elastic
Creep
Shrinkage

## Slide 3: Axial shortening
Construction sequence

## Slide 4: Fintel, Ghosh, Iyengar (1986) : parameters
Elastic shortening
  Stress
  Reinforcement
  Young’s modulus of concrete
  Concrete density
  Concrete strength
  Time
Shrinkage
  Drying / residual shrinkage
  Water content of concrete
  Member volume to surface area ratio
  Relative humidity
  Time
Creep
  True / drying / residual creep
  Stress
  Age of concrete at loading
  Member volume to surface area ratio
  Relative humidity
  Specific creep
  Concrete strength
  Time

## Slide 6: Why does it matter?
Partitions
Building services
Tolerances
Floor to ceiling heights
Overall building height

## Slide 7: Shard : structure
Steel
Concrete
Steel
Concrete

## Slide 8: Shard : column presets

## Slide 9: Shard : axial shortening records
Chart: 
| 40197 | 40218 | 40224 | 40233 | 40240 | 40248 | 40256 | 40281 | 40289 | 40298 | 40308 | 40318 | 40336 | 40358 | 40371 | 40388 | 40407 | 40434 | 40455 | 40464 | 40477 | 40487 | 40501 | 40513 | 40527 | 40548 | 40576 | 40606 | 40633 | 40654 | 40679 | 40737 | 40815 | 40934 | 40983 | 41039
L00 | -8 | -2 | 1 | 3 | 4 | 4 | 6 | 5 | 6 | 4 | 4 | 9 | 9 | 8 | 11 | 15 | 11 | 12 | 20 | 16 | 17 | 16 | 19 | 21 | 18 | 19 | 19 | 22 | 22 | 19 | 20 | 20 | 22 | 25 | 23 | 25
L10 | 0 | 0 | 0 | 0 | 4 | 3 | 6 | 20 | 16 | 17 | 25 | 20 | 22 | 22 | 24 | 25 | 24 | 23 | 23 | 27 | 27 | 23 | 24 | 26 | 29 | 32 | 30 | 32
L30 | 11 | 12 | 20 | 16 | 19 | 22 | 25 | 25 | 25 | 23 | 23 | 26 | 29 | 25 | 26 | 30 | 35 | 36 | 36 | 37
L50 | 5 | 7 | 8 | 10 | 8 | 8 | 13 | 17 | 11 | 12 | 18 | 32 | 31 | 33 | 35

## Slide 10: Shard : axial shortening records
Level | Date cast | Monitoring start | Delay
0 | 22/01/10 | 04/03/10 | 6 weeks
10 | 12/02/10 | 25/03/10 | 6 weeks
30 | 30/05/10 | 31/08/10 | 13 weeks
50 | 28/09/10 | 03/11/10 | 5 weeks
08/02/10
22/03/10

## Slide 11: Principal Place

## Slide 12: Axial shortening in high rise buildings
Cambridge CSIC
John Parker
09.09.14