## Slide 1
Monitoring of sprayed concrete lining in tunnels
using distributed fibre optic sensors
Crossrail Liverpool Street Station
running tunnel
concourse tunnel
running tunnel
Notes: CSIC Template 2013

## Slide 2
Monitoring of sprayed concrete lining in tunnels
using distributed fibre optic sensors
Crossrail Liverpool Street Station
running tunnel
concourse tunnel
running tunnel

## Slide 3
Monitoring of sprayed concrete lining in tunnels
using distributed fibre optic sensors
Crossrail Liverpool Street Station
Liverpool Street station
12 cross passages
~7700 m3 thickening concrete

## Slide 4
Monitoring of sprayed concrete lining in tunnels
using distributed fibre optic sensors
Additional stresses in the SCL due to cross passages
Cost savings
in SCL tunnels
Real data
Crossrail Liverpool Street Station

## Slide 5: Monitoring solution
Distributed fibre optics
CH5
CP2
CP1
Liverpool Street station
~800 m
embedded & exposed
fibre optic cables
Distributed
strain and temperature measurement

## Slide 6: Monitoring solution
Distributed fibre optics
First of its kind!

## Slide 7: Some results to date
Evolution of longitudinal strain
CP1 breakout and pilot tunnel
CP2 breakout and pilot tunnel
CP1 enlargement
June
July
compression
tension

## Slide 8: Some results to date
CP1 breakout and pilot tunnel
CP2 breakout and pilot tunnel
CP1 enlargement
June
July
Evolution of hoop strain
compression
tension

## Slide 9: Some results to date
Engineering insights
compression
tension

## Slide 10: Some results to date
Engineering insights
compression
tension

## Slide 11: Some results to date
Engineering insights
Plan view of typical enlargement chamber
compression
tension

## Slide 12: Conclusion
SC tunnel linings
 potentially large savings
Distributed fibre optics
 complete strain (& temperature) profile

## Slide 13
www.centreforsmartinfrastructure.com
Nicky de Battista
n.debattista @ eng.cam.ac.uk